PRODUCT   INFORMATION

AGS 3502 - TIXO, ANTI-GRAFFITI PROTECTIVE COATING

AGS 3502-TIXO

- Is a water based, weatherproof, long-term protective coating that can be applied to most surfaces.

- It is tixotropic  (liquid at stirring - jelly-like after applying) and can be used on smooth non-porous surfaces and high-porous surfaces, e.g. plastered surfaces, wood in the white, Light concrete and other surfaces.

- Spray-, brush- or roller applied graffiti can not penetrate AGS 3502-TIXO.

AGS 3502-TIXO

- AGS 3502-TIXO has exceptionally resistance to Indian ink and mechanical action.

- Applied in the right way it protects the surface for about 5 years.

- It protects the treated surface against air pollution, frost and moisture for about 5 years.

- Evaporation through AGS 3502-TIXO can take place.

- It is a sacrificial protection, which means that it has to be applied again after removal of the graffiti.

PROCEDURE

Preparations

First the surface has to be cleaned dirt, e.g. graffiti, traffic dirt etc.

Windows must be screened.

In case of protection of a new Building made of bricks, a plastered surface or a Building where the joints are newly repaired it may be necessary to lower pH on the surface before AGS 3502-TIXO is applied.

pH has to be less than 9 (use universal litmus paper).

To lower the pH BPS 7315 can be used.

Afterwards you rinse the surface with clean water to remove all chemicals.

The ideal air temperature is for applying is 10°- 35°C. The lower temperature in the autumn is 5°C. In spring it is 10ºC.

The humidity of the air must not exceed 95%.

Protection out of doors

AGS 3502-TIXO must be stirred before use.

Applied with low-pressure sprayer, brush or a roller.

Two coatings must be applied.

The first coating must dry 2-4 hours before the second coating is applied.

AGS 3502-TIXO can be applied on a surface that is not completely dry, just "handdry". That is when you put your hand on the surface there must not be drops of water on the palm when you remove it from the surface.

Protection indoor

On painted surfaces AGS 3502-TIXO is best applied with a window washer, but it can also be applied with a sponge, brush or roller combined with a window washer.

Two coating must be applied.

Cleaning of graffiti out of doors

Method 1: Normal surface:

Wash down the graffiti with a high-pressure cleaner: 90°C, 90 - 150 bar.

Be aware of loss of heat in the high-pressure cleaner at low temperatures.

In difficult cases use an AGS graffitiremover.

Then the surface has to be protected with two coatings of

AGS 3502-TIXO.

Method 2: A delicate surface

Let 90° - 95°C hot water run down over the graffiti.

As the graffiti is rinsed down the jet of water follows the graffiti down the surface.

If this method does not work, AGS 221, 221 Light, 521 or 560 are applied on the graffiti.

Let it work a couple of minutes.

Wash down the graffiti with a high-pressure cleaner, 90°C, 50 - 80 bar.

The method is especially very suitable when the surface is very weak.

Cleaning of graffiti indoors

Painted surfaces:

Apply hot water on the surface - more than 60°C - and wipe the graffiti of with a rag.

If this method does not work, apply AGS 221, 221 Light, 521 or 560 with a rag on the graffiti.

This must be done with caution in order not to ruin the paint.

Then the surface is cleaned with water.

If there is much graffiti washed down with a high-pressure cleaner with a mini-scrub and a water suction pump.

Then the surface has to be protected with two coatings of

AGS 3502-TIXO.

Porous surfaces:

Use a high-pressure cleaner with a mini-scrub and a water suction pump.

Then the surface has to be protected with two coatings of

AGS 3502-TIXO.

Reprotection of the surface

When the graffiti is removed from a protected surface, in most cases the protecting coating is also removed.

Reprotection has to be carried out with a minimum of two coatings of AGS 3502-TIXO.

The dose

AGS 3502-TIXO is never diluted.

Consumption

Consumption depends on characteristics, porosity, capilarity, smooth or irregular of the surface.

Concrete, brick and the like: 0,10 - 0,15 litre/m² pr. coating.

On sandstone, plaster, wood in the white and other very porous surfaces: 0,15 - 0,20 litre/m² pr. coating.

It is very important that you do not use less than 0,15 litre/m² pr. coating, as the protection then will be too thin to resist the more aggressive paints.

Time to dry

The protected surface repels water after about 2 hours.

It is dry after about 4 hours and hardened after about 72 hours.

Danger marking

On the 16th of May ALTox a/s has appraised that the AGS 3502-TIXO does not have to have a danger symbol.

As a service to the users a Safety Data Sheet is produced even when it is not a demand in the rules from Directorate for Arbejdstilsynet.

Code number

00-3 (1993).

Personal protective equipment

- Applying with brush, roller or window washer: Gloves.

- Applying with sprayer:

A breathing apparatus with an independent source of air, overall dress, gloves and a hood.

- Removal of the graffiti with a hotwater high-pressure cleaner: Waterproof dress, gloves and goggles.

A halfmask with a particle filter (minimum P2) is recommended.

Physical and chemical properties

Appearance:			White liquid.

Odour:			Weak odour

pH:				App. 8.

Density kg/l:			0,99.

Boiling point:		100(C.

Flash point:			82°C.

Solubility in water:		100%.

Dry matter:			10,5%

Packing:			10 and 25 litres plastic cans.

Characteristics

Transparent, more or less visible, dependant of the surface.

UV-resistent.

Protects against graffiti, pollution, frost and moisture.

OBS!	Some materials may get a little darker shade or the gloss may be increased al little.

Storage

Must be stored non-freezing in the original packing.

Durability

About 12 months in the original packing.

Transport information

The product is not considered as hazardous according to any transportation regulation.

This PRODUKT  INFORMATION is only intended as an information to the Contractor who uses the product. LTL can not give any guarantee for the result. The Contractor will have to carry out a test on the surface and be responsible for the result.

LTL ANTI GRAFFITI SYSTEM APS  (  SKOVVEJ 28  (  3230 GRÆSTED

TLF:+45 48792746 & +45 48792740  (  FAX:+45 48792747  ( BILTLF  +45 40732746 & +45 26702630